Section Cover Page

Section 07 11 13 2011-08-15 Bituminous Dampproofing

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

Use this Section to provide a barrier against moisture transport by capillary action, normally applied to concrete foundations above the water table, where no hydrostatic pressure is anticipated.  Where water under hydrostatic pressure is anticipated, specify waterproofing under a separate Section.

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Reference Documents

1.3	Submittals

1.4	Quality Assurance

1.5	Delivery, Storage, and Handling

2.	Products

2.1	Materials

2.2	Accessories

3.	Execution

3.1	Protection of Existing Work

3.2	Examination

3.3	Preparation

3.4	Application

3.5	Cleaning

LEED Notes:

With LEED certification there is no requirement for products applied to the exterior of a building to have restrictions on VOC content because it does not affect indoor air quality.

However, in order to follow sustainable building practices, specify emulsion type dampproofing instead of solvent type because emulsions have significantly less VOC content.

LEED Credits:

Contribution towards potential LEED credits may be available in this section:

.1	Some products have recycled content which will contribute to MR 4 – Recycled Content.

.2	Some products are manufactured regionally which may contribute to MR 5 – Regional Materials.

1.	General

1.1	RELATED Work Specified in Other SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16.]

.2	[LEED Requirements	Section 01 35 18.]

.3	[Environmental Procedures	Section 01 35 20.]

.4	Waste Management and Disposal	Section 01 74 19.

.5	[         ] waterproofing:	Section [            ].

.6	Perimeter insulation:	Section [            ].

1.2	REFERENCE documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED requirements and sustainable practices.

.1	American Society for Testing and Materials (ASTM):

| .1 | ASTM D1227-95 (2007) | Standard Specification for Emulsified Asphalt Used as a Protective Coating for Roofing |
| --- | --- | --- |
| .2 | ASTM D4479-07 | Standard Specification for Asphalt Roof Coatings - ;Asbestos-Free |
| .3 | ASTM D4586-07 | Standard Specification for Asphalt Roof Cement, Asbestos-Free |

.2	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org] |
| --- | --- | --- |

1.3	submittals

.1	Comply with requirements of Division 01.

.2	Product Data:

.1	Submit manufacturer's printed product literature, specifications and data sheet in accordance with Section 01 33 00 - Submittal Procedures.

.1	Provide [two] [         ] copies of most recent data sheets describing materials' physical properties and include product characteristics, performance criteria, physical size, finish and limitations.

.2	Provide [two] [           ] copies of MSDS for all products and indicate VOC content.

SPEC NOTE:  Use below paragraph for LEED projects when submittals are required.

.2	Sustainable Design Submittals:

SPEC NOTE:  Delete submittal item if project is not to attain LEED certification or if Credit MR 4 is not being sought.

.1	LEED Submittals: submit LEED submittal forms for Credit MR 4 in accordance with Section 01 32 16 LEED Submittal Forms and Section 01 35 18 LEED Requirements and the following:

.1	Recycled Content:  provide listing of products incorporating recycled content.  Include details of percentages of post-consumer and pre-consumer recycled content for materials and products.  Indicate material and product costs.

SPEC NOTE: Delete LEED submittal item if project is not to attain LEED certification or if Credit MR 5 is not being sought.

.2	LEED Submittals: submit LEED submittal forms for Credit MR 5 in accordance with Section 01 32 16 LEED Submittal Forms and Section 01 35 18 LEED Requirements and the following:

.1	Regional Materials: provide evidence that project incorporates required percentage [20] [30] % of regional materials/products, showing their cost, distances from extraction to manufacture and manufacture to project site, and total cost of materials for project.

1.4	Quality Assurance

.1	Mock-Ups:

SPEC NOTE:  Include this article only for large projects.

.1	Apply dampproofing to minimum 3 m x 3 m area, for approval.  Locate mock-up where directed by Minister.

.2	Materials and/or installation methods will be rejected if bond coverage or failure occurs.

.3	Clean rejected test areas free of applied finish, acceptable for new application.

1.5	DELIVERY, STORAGE, AND HANDLING

.1	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 - Management and Disposal.

2.	Products

2.1	MATERIALS

.1	Emulsion Type Dampproofing Coating:  Asphaltic, water based emulsion dampproofing, asbestos free, designed for application to exterior side of below grade foundations and walls, containing no solvents in accordance with ASTM D1227 and as follows:

.1	Application Temperature: 10°C

.2	Grade: [Spray   Type III or II, Class 1] [Brush   Type II, Class 1] [Trowel   Type II, Class 1].

.3	VOC Content: Maximum 30 g/L (less water and exempt solvents).

.2	Cutback Type Dampproofing Coating: Asphaltic, solvent based dampproofing, asbestos free, designed for application to exterior side of below grade foundations and walls in accordance with [ASTM D4479] [ASTM D4586] and as follows:

.1	Application Temperature: 2°C

.2	Grade: [Spray   Type I] [Brush   Type I] [Trowel   Type I, Class 1].

.3	VOC Content: maximum 250 g/l.

2.2	accessories

.1	Joint Sealing Compound:  as recommended by dampproofing manufacturer.

.2	Primer: as recommended by dampproofing manufacturer.

.3	Patching Compound: fibred mastic compound as recommended by dampproofing manufacturer.

.4	Reinforcing fabric: asphalt coated fabric as recommended by dampproofing manufacturer.

3.	Execution

3.1	PROTECTION

.1	Protect adjoining surfaces from soiling during application.

3.2	examination

.1	Examine substrates and verify that surface smoothness, moisture emissions and other conditions affecting performance of materials specified in this Section complies with the dampproofing manufacturer’s recommended substrate requirements.

3.3	preparation

.1	Protect and mask adjoining exposed surfaces from being stained, spotted or coated with dampproofing; prevent dampproofing materials from entering or clogging weep holes, drains and perimeter drainage systems.

.2	Seal exterior joints between foundation walls and footings, joints between concrete floor slab and foundation and around penetrations through dampproofing with sealing compound and reinforcing fabric before applying dampproofing.

.3	Clean substrates, remove projections; fill voids and apply bond breakers (if required), and apply primer as recommended by dampproofing manufacturer

3.4	APPLICATION

.1	Apply dampproofing to provide a continuous, uniform coating to entire exterior faces of foundation walls from 50 mm below finish grade level to and including tops of foundation wall footings:

.1	Do not permit dampproofing to extend onto surfaces exposed to view in final construction.

.2	Reinforce changes in direction greater than 45° at intersections, projecting surfaces, internal and external corners, changes in plane, and across construction joints, cracks and honeycombing; apply additional coat of dampproofing material to embed reinforcing fabric into primary dampproofing membrane; extend reinforcing fabric 200 mm to each side of areas requiring reinforcing.

.3	Allow for additional coats to achieve required coating.

.4	Provide sufficient drying time between successive coatings.

.5	Provide drying time according to manufacturer’s recommendations before backfilling.  Allow for a range of ambient temperatures and humidity.

.3	Use cutback asphalt materials at temperatures below 5°C.

.4	Use either cutback or emulsified asphalt materials, at Contractor's option, when surfaces and ambient air will be minimum 5°C for 72 hours before application, during application and for curing period.

.5	Seal holes around pipes and other services passing through dampproofed surfaces by using joint sealing compound applied in accordance with manufacturer's directions.

3.5	cleaning

.1	Dampproofing materials shall be removed from surfaces not intended to receive dampproofing.

END OF SECTION