Section Cover Page

Section 07 13 00 2011-08-15 Sheet Membrane Waterproofing

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Reference Documents

1.3	Product Options and Substitutions

1.4	Submittals

1.5	Quality Assurance

1.6	Delivery, Storage, and Handling

1.7	Site Conditions

2.	Products

2.1	Materials

3.	Execution

3.1	Examination

3.2	Preparation

3.3	Application/Workmanship

LEED Notes:

With LEED certification there is no requirement for products applied to the exterior of a building to have restrictions on VOC content because it does not affect indoor air quality.

However, in order to follow sustainable building practices, specify water-based primer instead of solvent type because water-based have significantly less VOC content.  Cautionary note: water-based primers are restricted in their use depending upon ambient temperature at application. Time of year may dictate type of primer that can be used.

LEED Credits:

Contribution towards potential LEED credits may be available in this section:

.1	Some products have recycled content which will contribute to MR 4 – Recycled Content.

.2	Some products are manufactured regionally which may contribute to MR 5 – Regional Materials.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16.]

.2	[LEED Requirements	Section 01 35 18.]

.3	[Environmental Procedures	Section 01 35 20.]

.4	Waste Management and Disposal	Section 01 74 19.

.5	Concrete substrate:	Section 03 30 00.

.6	Waterproofing/dampproofing:	Section [            ].

.7	Rigid insulation cover:	Section 07 21 13.

.8	Sealants:	Section 07 92 00.

1.2	REFERENCE documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED requirements and sustainable practices.

.1	American Society for Testing and Materials (ASTM):

| .1 | ASTM D36-06 | Standard Test Method for Softening Point of Bitumen (Ring-and-Ball Apparatus) |
| --- | --- | --- |
| .2 | ASTM D146-04 | Standard Test Methods for Sampling and Testing Bitumen-Saturated Felts and Woven Fabrics for Roofing and Waterproofing |
| .3 | ASTM D2523-00 (2006) | Standard Practice for Testing Load-Strain Properties of Roofing Membranes |
| .4 | ASTM E96/E96M-05 | Standard Test Methods for Water Vapor Transmission of Materials |

.2	Canada Green Building Council (CaGBC):

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org] |
| --- | --- | --- |

.3	Canadian General Standards Board (CGSB):

| .1 | CAN/CGSB 37-GP-9Ma | Primer, Asphalt, Unfilled, for Asphalt Roofing, Dampproofing and Waterproofing |
| --- | --- | --- |

1.3	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.4	submittals

.1	Comply with requirements of Division 01.

.2	Product Data:

.1	Submit manufacturer's printed product literature, specifications and data sheet in accordance with Section 01 33 00 - Submittal Procedures.

.2	Provide [two] [          ] copies of most recent technical waterproofing components data sheets describing materials' physical properties and include product characteristics, performance criteria, physical size, finish and limitations.

.3	Provide [two] [          ] copies of MSDS for all products and indicate VOC content for primer.

SPEC NOTE:  Use below paragraph for LEED projects when submittals are required.

.2	Sustainable Design Submittals:

.1	LEED Submittals: Co-ordinate submittals requirements in accordance with Section 01 35 18 - LEED Requirements.

SPEC NOTE:  Delete submittal item if project is not to attain LEED certification or if Credit MR 4 is not being sought.

.2	LEED Submittals: submit LEED submittal forms for Credit MR 4 in accordance with Section 01 32 16 LEED Submittal Forms and Section 01 35 18 LEED Requirements and the following:

.1	Recycled Content:  provide listing of products incorporating recycled content.  Include details of percentages of post-consumer and pre-consumer recycled content for materials and products.  Indicate material and product costs.

SPEC NOTE: Delete LEED submittal item if project is not to attain LEED certification or if Credit MR 5 is not being sought.

.3	LEED Submittals: submit LEED submittal forms for Credit MR 5 in accordance with Section 01 32 16 LEED Submittal Forms and Section 01 35 18 LEED Requirements and the following:

.1	Regional Materials: provide evidence that project incorporates required percentage [20] [30] % of regional materials/products, showing their cost, distances from extraction to manufacture and manufacture to project site, and total cost of materials for project.

1.5	quality assurance

.1	Testing Agencies

SPEC NOTE:  Use clauses for large or involved projects.

.1	Provide necessary facilities and co-operate with inspection firm engaged and paid for by the Minister.

.2	Construct a panel [          ] m2 minimum of typical waterproofing installation, for approval.  Locate where directed.

.3	The work will be rejected if the specified criteria is not met.

.4	Clean rejected test areas free of applied finish, acceptable for new application.

1.6	DELIVERY, Storage, and handling

.1	Delivery and Acceptance Requirements:

.1	Deliver and store materials, undamaged in original wrappings, in a suitable environment.

.2	Storage and Handling Requirements:

.1	Provide adequate protection of materials and work of this section from damage by weather and other causes.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 - Management and Disposal.

1.7	Site conditions

.1	Maintain surfaces and ambient air temperature 5°C minimum, for a minimum period of 72 hours prior to, during, and after waterproofing application.

2.	Products

2.1	MATERIALS

SPEC NOTE:  Specify water-based primer when possible to follow sustainable building practices.

.1	Primer:  to CGSB 37-GP-9Ma.[proprietary to membrane product and water-based].

.2	Waterproofing Membrane:  Pressure sensitive sheet consisting of rubberized asphalt 1.5 mm thick bonded to 250 micrometre thick polyethylene; conforming to the following properties:

Colour:	black

Thickness (total):	1.8 mm

Water vapour transmission:	ASTM E96-95/E96M Method B

0.003 metric perms

Tensile Strength:	ASTM D2523

13,800 kPa

Softening Point:	ASTM D36-06 38°C

Pliability:	ASTM D146– 0-25°C

.3	Slip Sheet:  Waterproofing membrane specified above but with the polyethylene bond breaker sheet left intact and not stripped from membrane.

.4	Mastic:  for sealing joints and edges of membrane use rubberized asphalt [similar material specified for membrane] in gun grade.

3.	Execution

3.1	EXAMINATION

.1	Ensure concrete surfaces are clean, dry, smooth and free of fines, voids, honeycomb, etc.

.2	Surfaces shall be free from loose particles, grease, oil and other foreign matter.

.3	Fill holes and cracks and ensure continuity of flat surface.

.4	All concrete surfaces shall be surface dry and have negative alkalinity when surface tested.

.5	Ambient surfaces and material temperature shall be minimum 5°C.

3.2	preparation

.1	Protect the work of other trades from damage resulting from work of this Section.  Make good such damage to the satisfaction of the Minister.

3.2	APPLICATION/WORKMANSHIP

.1	Apply primer at a rate of 6 to 16 m2/L depending on porosity of surface.

.2	Seal holes around pipes and other services passing through membrane by using mastic applied in accordance with manufacturer's directions.

.3	Allow primer to dry one hour or until tack free, but not more than 36 hours prior to application of membrane.

.4	Reapply primer if time lapsed between first application and installation of membrane exceeds 36 hours.

.5	Apply membrane in continuous strips, to as long length as possible to minimize joints.  Stagger 914 mm and 305 mm widths in accomplishing 1219 mm width; seal butted edges with 150 mm width of membrane.

.6	Lap all ends 65 mm minimum.  Seal all seams with mastic, applied in accordance with manufacturer's written instructions.

.7	All inside and outside corners shall be double covered with initial strip of membrane 457 mm wide, centered.

.8	Construction and control joints:  double ply covered with initial strip of 150 mm width and second strip of 457 mm width, after application of dampproofing.

.9	Expansion joints:  triple ply with initial strip of 229 mm width (applied adhesives side out), second strip of 457 mm wide final layer of 914 mm width; after application of any sealant or dampproofing materials.

.10	Cut-off at end of day operations shall be sealed with 150 mm wide strip set in mastic.

.11	Areas around drains, piping, vents, etc. shall be liberally coated with mastic before and after application of membrane.

.12	Refer to manufacturer's written instructions and details for required procedures of installation.

.13	At all locations where membrane will be covered with insulation, temporarily protect membrane from puncture or install membrane immediately prior to application of insulation.

END OF SECTION