Section Cover Page

Section 09 91 25 Interior Repainting and 2014-11-01 Refinishing Schedule

Use this Section to schedule finish systems for all previously finished, interior substrates requiring site painting and finishing, except mechanical and electrical work.

The Infrastructure, Basic Master Specification contains the following series of Sections that specify site painting and finishing:

.1	Section 09 91 05 - Painting and Finishing General Requirements

.2	Section 09 91 13 - Exterior Painting and Finishing Schedule

.3	Section 09 91 15 - Exterior Repainting and Refinishing Schedule

.4	Section 09 91 23 - Interior Painting and Finishing Schedule

.5	Section 09 91 25 - Interior Repainting and Refinishing Schedule (this Section)

.6	Section 09 91 30 - Painting of Mechanical and Electrical Work

These sections are interrelated.  Section 09 91 05 specifies general requirements while the remaining Sections in the series specify finish systems, i.e. specific products and number of coats, required for various types of substrates.  Always include Section 09 91 05.  Include one or more of the remaining Sections only to the extent they are applicable to the project.

This Master Specification Section contains:

.1	This Cover Sheet

.2	Data Sheet - General

.3	Specification Section Text:

1.	General

1.1	Intent

2.	Products

(Not used)

3.	Execution

3.1	Interior Repainting and Refinishing Schedule

This Section includes a comprehensive listing of previously finished, interior, substrates complete with MPI code numbers, finishing system descriptions and product descriptions.

The individual finish systems listed in this master schedule must be edited to suit the project.  Note that the schedule generally calls for repainting and refinishing with 2 coats, after priming to suit the degree of deterioration.  Two coats are recommended if a high quality result is desired.  If repainting/refinishing with a single coat is deemed adequate, or if project budget does not permit two coats, the schedule must be edited accordingly.

Specifier has the option of scheduling painting and finishing by one of two methods:

.1	Method #1:  Indicate in Room Finish Schedule, Door and Frame Schedule, and elsewhere as required, the proper code designation and where applicable, gloss level, of the required finish system for each item or substrate that requires site painting or finishing.  In this Section, specify the finish system corresponding to each required finish.  Coordinate with Room Finish Schedule, Door and Frame Schedule, etc.

.2	Method #2:  Incorporate a comprehensive listing of each item or substrate that requires site finishing into this Section.  Do not indicate code designations elsewhere.  Since this Section describes substrate elements in general terms only, mainly for reference purposes, it may require modification and expansion to include more specific and detailed substrate descriptions.  Use this option for small, simple projects only.

Carefully consider all surfaces to be repainted or refinished and ensure that appropriate finishing systems are specified for each surface type. Review the system evaluation and surface preparation sections of the MPI Maintenance Repainting Manual when selecting finishing systems.

Specify only those finishing systems that are applicable to the project. Delete all other finishing systems.

END OF DATA SHEET

1.	General

1.1	INTENT

.1	Read this Section in conjunction with Section 09 91 05 - Painting and Finishing General Requirements.

2.	Products

.1	(Not used).

- Execution

3.1	INTERIOR PAintING AND FINISHING SCHEDULE

.1	The following systems with codes numbers, finishing system description, gloss levels, coats and product descriptions are derived from the MPI Maintenance Repainting Manual and the MPI Approved Products List.

.2	Prime substrate, referencing the 1st coat, for the Degree of Surface Deterioration codes as recommended by the MPI Maintenance Repainting Manual and as follows:

.1	DSD 1:  Touch-up.

.2	DSD 2:  Spot prime.

.3	DSD 3:  Full prime coat.

.3	Where the finishing system requires different product for first coat, DSD 1, 2 or 3, the MPI product numbers will be noted in the finishing system description.

SPEC NOTE: Where more than one product number is specified with the finishing system description, refer to MPI Maintenance Repainting Manual to determine which product suits project requirements.

SPEC NOTE: Delete finishing systems as required to include only systems required for the project. Edit all option fields.  Where more than one Gloss Level is required for a particular substrate, include all applicable gloss levels and ensure location of various gloss levels are clearly defined in Section 09 91 05, Article 2.4, Paragraph 2.4.2

# RIN 2.1 – ASPHALT SURFACES

| RIN 2.1A | Latex Zone / Traffic Marking | Latex Zone/Traffic Marking Paint, Apply in strict accordance with manufacturer’s instructions. |
| --- | --- | --- |
| RIN 2.1B | Alkyd Zone / Traffic Marking | Alkyd Zone/Traffic Marking Paint, Apply in strict accordance with manufacturer’s instructions. |

RIN 3.1 – CONCRETE VERTICAL SURFACES

| RIN 3.1A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 3 – MPI # 50) | 3rd | Latex |
| RIN 3.1B | Latex Aggregate | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
|  | [Coarse] [Medium] texture, |  |
|  | Gloss level [G1] [G5] [G6] |  |
| RIN 3.1C | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| RIN 3.1D | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 50) | 3rd | Alkyd |
| RIN 3.1E | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 3.1F | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 3.1G | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 125) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 3.1H | Water Repellent | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (paintable) |  |
| RIN 3.1J | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  | Gloss level [G2] [G3] [G4] [G5] | 2nd | HIPAC Latex |
|  | (DSD 3 –MPI # 50) | 3rd | HIPAC Latex |
| RIN 3.1K | Concrete Stain | Concrete Stain, Apply in strict accordance with manufacturer’s instructions. |
| RIN 3.1L | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 3 –MPI # 50) | 3rd | Institutional Low Odor / VOC |

RIN 3.2 – CONCRETE HORIZONTAL SURFACES

| RIN 3.2A | Latex Floor Enamel | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G3] [G6] | 2nd | Latex Floor |
|  |  | 3rd | Latex Floor |
| RIN 3.2B | Alkyd Floor Paint | 1st | DSD [1] [2] [3] |
|  | Gloss level [G4] [G6] | 2nd | Alkyd Floor |
|  |  | 3rd | Alkyd Floor |
| RIN 3.2C | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 3.2D | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 3.2E | Concrete Floor Sealer | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Concrete Floor Sealer |
|  |  | 3rd | Concrete Floor Sealer |
| RIN 3.2F | Concrete Floor Sealer, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Concrete Floor Sealer |
|  |  | 3rd | Concrete Floor Sealer |
| RIN 3.2G | Latex Zone / Traffic Marking | Latex, Apply in strict accordance with manufacturer’s instructions. |
| RIN 3.2H | Alkyd Zone / Traffic Marking | Alkyd, Apply in strict accordance with manufacturer’s instructions. |
| RIN 3.2J | Concrete Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Concrete Stain |
|  |  | 3rd | Concrete Stain |
| RIN 3.2K | Polyurethane, Clear, 2 Component | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
|  |  | 4th | Polyurethane |
| RIN 3.2L | Epoxy Floor Paint, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | W. B. Epoxy Floor Paint |
|  |  | 3rd | W. B. Epoxy Floor Paint |
|  |  | 4th | W. B. Epoxy Floor Paint |

RIN 3.3 – CEMENTITIOUS COMPOSITION BOARD

| RIN 3.3A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 3 – MPI # 50) | 3rd | Latex |
| RIN 3.3B | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 3 – MPI # 50) |  |  |
| RIN 3.3C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 50) | 3rd | Alkyd |
| RIN 3.3D | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 3.3E | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 3.3F | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 125) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 3.3G | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 3 – MPI # 50) | 3rd | Institutional Low Odor / VOC |
| RIN 3.3H | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |

RIN 4.1 – CLAY MASONRY UNITS

| RIN 4.1A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 3 – MPI # 50) | 3rd | Latex |
| RIN 4.1B | Latex Aggregate, | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
|  | [Coarse] [Medium] texture, |  |
|  | Gloss level [G1] [G5] [G6] |  |
| RIN 4.1C | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| RIN 4.1D | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 50) | 3rd | Alkyd |
| RIN 4.1F | Epoxy | 1st | DSD [1] [2] [3] |
|  | (for smooth brick) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 4.1G | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  | (for smooth brick) | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 4.1H | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 125) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 4.1J | Water Repellent, Clear | Water Repellent, Apply in strict accordance with manufacturer’s instructions |
|  | (paintable) |  |
| RIN 4.1K | Polyurethane, Clear, 2 Component | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 4.1L | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 3 – MPI # 50) |  |  |
| RIN 4.1M | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 3 – MPI # 50) | 3rd | Institutional Low Odor / VOC |

RIN 4.2 – CONCRETE MASONRY UNITS (block and brick)

| RIN 4.2A | Latex, | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 3 – MPI # 50) | 3rd | Latex |
| RIN 4.2B | Latex Aggregate, | Latex Aggregate, Apply in strict accordance with manufacturer’s instructions. |
|  | [Coarse] [Medium] texture, |  |
|  | Gloss level [G1] [G5] [G6] |  |
| RIN 4.2C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 50) | 3rd | Alkyd |
| RIN 4.2D | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 4.2E | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 125) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 4.2F | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 4.2G | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  |  | 3rd | W. B. Light Industrial Coating |
| RIN 4.2H | Water Repellent | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (not paintable) |  |
|  | (do not use on low density block) |  |
| RIN 4.2J | Water Repellent | Water Repellent, Apply in strict accordance with manufacturer’s instructions. |
|  | (paintable) |  |
|  | (do not use on low density block) |  |
| RIN 4.2K | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC |
|  | (DSD 3 – MPI # 50) |  |  |
| RIN 4.2L | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 3 – MPI # 50) | 3rd | Institutional Low Odor / VOC |

RIN 5.1 – STRUCTURAL STEEL & METAL FABRICATIONS

| RIN 5.1A | Quick Dry Enamel | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G5] [G6] | 2nd | Quick Dry Enamel |
|  | (DSD 2 or 3 – MPI # [76] [95]) | 3rd | Quick Dry Enamel |
| RIN 5.1B | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 107) | 3rd | W.B. Light Industrial Coating |
| RIN 5.1C | Latex Dry Fall | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [79] [95]) | 2nd | Latex Dry Fall |
| RIN 5.1D | Alkyd Dry Fall | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [79] [95]) | 2nd | Alkyd Dry Fall |
| RIN 5.1E | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [23] [79]) | 3rd | Alkyd |
| RIN 5.1F | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 101) | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 5.1G | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (over high build epoxy) | 2nd | Polyurethane |
|  | (DSD 2 or 3 – MPI # [101], [98] [108] as required) | 3rd | Polyurethane |
| RIN 5.1H | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (over epoxy) | 2nd | Polyurethane |
|  | (DSD 1, 2 or 3 – MPI # [18] [20], [77] as required) | 3rd | Polyurethane |
| RIN 5.1J | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 107) | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 5.1K | Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 101) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 5.1L | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [23] [79]) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| RIN 5.1M | Multicolour | 1st | DSD [1] [2] [3] |
|  | (DSD 1 – MPI # 125) | 2nd | Multicolour Base Coat |
|  | (DSD 2 or 3 – MPI # [23] [79] [107]) | 3rd | Multicolour Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 5.1N | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [23] [79] [107]) | 3rd | Latex |
| RIN 5.1P | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 101) | 3rd | W.B. Light Industrial Coating |
| RIN 5.1Q | High Build Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [18] [20], [98] [108] as required) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 5.1R | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [23] [79] [107]) |  |  |
| RIN 5.1S | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 107) | 3rd | Institutional Low Odor / VOC |

RIN 5.2 – STEEL – HIGH HEAT

| RIN 5.2A | Heat Resistant Enamel | Heat Resistant Enamel, Apply in strict accordance with Manufacturer’s Instructions |
| --- | --- | --- |
|  | Maximum 205°C (400°F) |  |
| RIN 5.2B | Heat Resistant Enamel, Aluminum | Aluminum Heat Resistant Enamel, Apply in strict accordance with Manufacturer’s Instructions |
|  | Maximum 427°C (800°F) |  |
| RIN 5.2C | Inorganic Zinc Rich Coating | Inorganic Zinc Rich Coating, Apply in strict accordance with Manufacturer’s Instructions |
|  | Maximum 400°C (750°F) |  |
| RIN 5.2D | High Heat Resistant Coating | High Heat Resistant Coating, Apply in strict accordance with Manufacturer’s Instructions |
|  | Maximum 593°C (1100°F) |  |

RIN 5.3 – GALVANIZED METAL (not chromate passivated)

| RIN 5.3A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [26] [134] [135]) | 3rd | Latex |
| RIN 5.3B | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # [26] [134] [135]) | 3rd | W.B. Light Industrial Coating |
| RIN 5.3C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [26] [134] [135]) | 3rd | Alkyd |
| RIN 5.3D | Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 –MPI # 101) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 5.3E | Alkyd Dry Fall | 1st | DSD [1] [2] [3] |
|  | (low contact / traffic) | 2nd | Alkyd Dry Fall |
|  | (DSD 2 or 3 – MPI # 26) |  |  |
| RIN 5.3F | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 26) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| RIN 5.3G | Latex Dry Fall | 1st | DSD [1] [2] [3] |
|  | (low contact / traffic) | 2nd | Latex Dry Fall |
|  | (DSD 2 or 3 – MPI # [26] [134] [135]) |  |  |
| RIN 5.3H | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 –MPI # 101) | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 5.1J | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [26] [134] [135]) |  |  |
| RIN 5.1K | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 134) | 3rd | Institutional Low Odor / VOC |

RIN 5.4 – ALUMINUM (non-anodized)

| RIN 5.4A | Alkyd | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 95) | 3rd | Alkyd |
| RIN 5.4B | Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 –MPI # 101) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 5.4C | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 –MPI # 101) | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 5.4D | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 95) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| RIN 5.4E | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 95) | 3rd | W.B. Light Industrial Coating |
| RIN 5.4F | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # 95) |  |  |
| RIN 5.4G | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 95) | 3rd | Institutional Low Odor / VOC |
| RIN 5.4H | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # 95) | 3rd | Latex |

RIN 5.5 – COPPER

| RIN 5.5A | Alkyd | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 3rd | Alkyd |
| RIN 5.5B | Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 101) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 5.5C | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 101) | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 5.5D | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| RIN 5.5E | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 3rd | W.B. Light Industrial Coating |
| RIN 5.5F | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [69] [95]) |  |  |
| RIN 5.5G | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 3rd | Institutional Low Odor / VOC |
| RIN 5.5H | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 3rd | Latex |

RIN 5.6 – STAINLESS STEEL (not polished)

| RIN 5.6A | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 69) | 3rd | W.B. Light Industrial Coating |
| RIN 5.6B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 3rd | Alkyd |
| RIN 5.6C | Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 101) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 5.6D | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 101) | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 5.6E | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| RIN 5.6F | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W.B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 95) | 3rd | W.B. Light Industrial Coating |
| RIN 5.6G | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [69] [95]) |  |  |
| RIN 5.6H | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [69] [95]) | 3rd | Latex |

RIN 6.1 – GLUE LAMINATED BEAMS AND COLUMNS

| RIN 6.1A | Latex, (over alkyd primer) | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | Latex |
| RIN 6.1B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | Alkyd |
| RIN 6.1C | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # [88] [102]) | 3rd | Alkyd Varnish |
| RIN 6.1D | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G6] | 2nd | Polyurethane Varnish |
|  |  | 3rd | Polyurethane Varnish |
| RIN 6.1E | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 6.1F | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G5] [G6] | 2nd | W. B. Acrylic |
|  |  | 3rd | W. B. Acrylic |
| RIN 6.1G | Semi-transparent Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Semi-transparent Stain |
| RIN 6.1H | Alkyd Solid Color Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Solid Color Wood Stain |
|  |  | 3rd | Solid Color Wood Stain |
| RIN 6.1J | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | W. B. Light Industrial Coating |
| RIN 6.1K | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 6.1L | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Alkyd Varnish |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.1M | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane Varnish |
|  | Gloss Level [G4] [G6] | 3rd | Polyurethane Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.1N | Fire Retardant Coating | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.1P | Latex, (over latex primer) | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # 39) | 3rd | Latex |
| RIN 6.1Q | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # 39) |  |  |
| RIN 6.1R | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 39) | 3rd | Institutional Low Odor / VOC |
| RIN 6.1S | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | W. B. Acrylic |
|  | Gloss Level [G4] [G5] [G6] | 3rd | W. B. Acrylic |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.1T | Polyurethane, Clear, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane |
|  | Gloss Level [G1] [G6] | 3rd | Polyurethane |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.1U | Latex Solid Color Stain | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [39] [46]) | 2nd | Latex Solid Stain |
|  |  | 3rd | Latex Solid Stain |

RIN 6.2 – DIMENSION LUMBER

| RIN 6.2A | Latex (over alkyd primer) | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 –MPI # 46) | 3rd | Latex |
| RIN 6.2B | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [39] [46]) |  |  |
| RIN 6.2C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 –MPI # 46) | 3rd | Alkyd |
| RIN 6.2D | Latex, (over latex primer) | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 –MPI # 39) | 3rd | Latex |
| RIN 6.2E | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 –MPI # 46) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 6.2F | Fire Retardant, Pigmented | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.2G | Fire Retardant, Clear | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.2H | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane Varnish |
|  | Gloss Level [G4] [G6] | 3rd | Polyurethane Varnish |
|  | (DSD 1, 2 or 3 –MPI # 90) |  |  |
| RIN 6.2J | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | W. B. Light Industrial Coating |
| RIN 6.2 K | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 6.2L | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # [88] [102]) | 3rd | Alkyd Varnish |
| RIN 6.2M | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G6] | 2nd | Polyurethane Varnish |
|  |  | 3rd | Polyurethane Varnish |
| RIN 6.2N | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Alkyd Varnish |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.2P | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 39) | 3rd | Institutional Low Odor / VOC |
| RIN 6.2Q | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | W. B. Acrylic |
|  | Gloss Level [G4] [G5] [G6] | 3rd | W. B. Acrylic |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.2R | Polyurethane, Clear, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane |
|  | Gloss Level [G1] [G6] | 3rd | Polyurethane |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.2S | Semi-transparent Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Semi-transparent Stain |

RIN 6.3 – DRESSED LUMBER

| RIN 6.3A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | (over alkyd undercoat) | 2nd | Latex |
|  | Gloss Level [G5] [G6] | 3rd | Latex |
|  | (DSD 2 or 3 – MPI # 46) |  |  |
| RIN 6.3B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | Alkyd |
| RIN 6.3C | Semi-transparent Stain | 1st | DSD [1] [2] [3] |
|  | (low contact / traffic) | 2nd | Wood Stain |
| RIN 6.3D | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Alkyd Varnish |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.3E | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane Varnish |
|  | Gloss Level [G4] [G6] | 3rd | Polyurethane Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.3F | Lacquer, Clear | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Lacquer Sanding Sealer |
|  | Gloss Level [G4] [G6] | 3rd | Clear Lacquer |
|  | (DSD 2 or 3 – MPI # 90) | 4th | Clear Lacquer |
| RIN 6.3G | Lacquer, Pigmented | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G5] [G6] | 2nd | Pigmented Lacquer |
|  | (DSD 2 or 3 – MPI # 24) | 3rd | Pigmented Lacquer |
| RIN 6.3H | Lacquer, Clear | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G6] | 2nd | Clear Lacquer |
|  | (DSD 2 or 3 – MPI # 84) | 3rd | Clear Lacquer |
|  |  | 4th | Clear Lacquer |
| RIN 6.3J | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # [88] [102]) | 3rd | Alkyd Varnish |
| RIN 6.3K | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G6] | 2nd | Polyurethane Varnish |
|  |  | 3rd | Polyurethane Varnish |
| RIN 6.3L | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 6.3M | Danish Oil | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Danish Oil |
| RIN 6.3N | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 46) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 6.3P | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | W. B. Light Industrial Coating |
| RIN 6.3Q | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G5] [G6] | 2nd | W. B. Acrylic |
|  |  | 3rd | W. B. Acrylic |
| RIN 6.3R | Fire Retardant, Pigmented | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.3S | Fire Retardant, Clear | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.3T | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [39] [46]) |  |  |
| RIN 6.3U | Latex | 1st | DSD [1] [2] [3] |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G5] [G6] | 3rd | Latex |
|  | (DSD 2 or 3 – MPI # 39) |  |  |
| RIN 6.3V | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 39) | 3rd | Institutional Low Odor / VOC |
| RIN 6.3W | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | W. B. Acrylic |
|  | Gloss Level [G4] [G5] [G6] | 3rd | W. B. Acrylic |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.3X | Polyurethane, Clear, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G6] | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 6.3Y | Polyurethane, Clear, 2 Component | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 6.3Z | Polyurethane, Clear, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane |
|  | Gloss Level [G1] [G6] | 3rd | Polyurethane |
|  | (DSD 2 or 3 – MPI # 90) |  |  |

RIN 6.4 – WOOD PANELING

| RIN 6.4A | Latex, | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | Latex |
| RIN 6.4B | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # 46) |  |  |
| RIN 6.4C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | Alkyd |
| RIN 6.4D | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 39) | 3rd | Institutional Low Odor / VOC |
| RIN 6.4E | Semi-transparent Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Wood Stain |
| RIN 6.4F | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Alkyd Varnish |
|  | Gloss Level [G1] [G5] [G6] | 3rd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.4G | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane Varnish |
|  | Gloss Level [G4] [G6] | 3rd | Polyurethane Varnish |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.4H | Lacquer, Clear | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Lacquer Sanding Sealer |
|  | Gloss Level [G1] [G4] [G6] | 3rd | Clear Lacquer |
|  | (DSD 2 or 3 – MPI # 90) | 4th | Clear Lacquer |
| RIN 6.4J | Alkyd Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G5] [G6] | 2nd | Alkyd Varnish |
|  | (DSD 2 or 3 – MPI # [88] [102]) | 3rd | Alkyd Varnish |
| RIN 6.4K | Lacquer, Pigmented | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G5] [G6] | 2nd | Pigmented Lacquer |
|  | (DSD 2 or 3 – MPI # 24) | 3rd | Pigmented Lacquer |
| RIN 6.4L | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G6] | 2nd | Polyurethane Varnish |
|  |  | 3rd | Polyurethane Varnish |
| RIN 6.4M | Danish Oil | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Danish Oil |
| RIN 6.4N | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 46) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 6.4P | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G4] [G5] [G6] | 2nd | W. B. Acrylic |
|  |  | 3rd | W. B. Acrylic |
| RIN 6.4Q | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # 46) | 3rd | W. B. Light Industrial Coating |
| RIN 6.4R | Fire Retardant, Pigmented | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.4S | Fire Retardant, Clear | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.4T | Latex | 1st | DSD [1] [2] [3] |
|  | (over latex primer) | 2nd | Latex |
|  | Gloss Level [G5] [G6] | 3rd | Latex |
|  | (DSD 2 or 3 – MPI # 39) |  |  |
| RIN 6.4U | Waterborne Acrylic, Clear | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | W. B. Acrylic |
|  | Gloss Level [G4] [G5] [G6] | 3rd | W. B. Acrylic |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.4V | Polyurethane, Clear, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane |
|  | Gloss Level [G1] [G6] | 3rd | Polyurethane |
|  | (DSD 2 or 3 – MPI # 90) |  |  |
| RIN 6.4W | Lacquer, Clear | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G4] [G6] | 2nd | Clear Lacquer |
|  | (DSD 2 or 3 – MPI # 84) | 3rd | Clear Lacquer |
|  |  | 4th | Clear Lacquer |

RIN 6.5 – WOOD FLOORS AND STAIRS

| RIN 6.5A | Alkyd Floor Enamel | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G4] [G6] | 2nd | Alkyd Floor Enamel |
|  |  | 3rd | Alkyd Floor Enamel |
| RIN 6.5B | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane Varnish |
|  | Gloss Level G6 | 3rd | Polyurethane Varnish |
|  | (DSD 2 or 3 – MPI # 90) | 4th | Polyurethane Varnish |
| RIN 6.5C | Polyurethane Varnish | 1st | DSD [1] [2] [3] |
|  | Gloss Level G6 | 2nd | Polyurethane Varnish |
|  |  | 3rd | Polyurethane Varnish |
|  |  | 4th | Polyurethane Varnish |
| RIN 6.5D | Polyurethane, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | Gloss Level G6 | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 6.5E | Alkyd Game Line Marking | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Alkyd |
| RIN 6.5F | Epoxy Game Line Marking | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
| RIN 6.5G | Polyurethane, Clear, 2 Component | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 6.5H | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Polyurethane |
|  |  | 3rd | Polyurethane |
| RIN 6.5J | Latex Porch & Floor Enamel | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G6] | 2nd | Floor Enamel |
|  | (DSD 2 or 3 – MPI # 45) | 3rd | Floor Enamel |
| RIN 6.5K | Epoxy Floor Paint, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | W. B. Epoxy Floor Paint |
|  |  | 3rd | W. B. Epoxy Floor Paint |
| RIN 6.5L | Polyurethane, Moisture Cured | 1st | DSD [1] [2] [3] |
|  | (over stain) | 2nd | Polyurethane |
|  | Gloss Level G6 | 3rd | Polyurethane |
|  | (DSD 2 or 3 – MPI # 90) | 4th | Polyurethane |

RIN 6.6 – WOOD SHINGLE AND SHAKE

| RIN 6.6A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # 45) | 3rd | Latex |
| RIN 6.6B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 45) | 3rd | Alkyd |
| RIN 6.6C | Semi-transparent Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Semi-transparent Stain |
| RIN 6.6D | Alkyd Solid Colour Stain | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Alkyd Solid Colour Stain |
|  |  | 3rd | Alkyd Solid Colour Stain |
| RIN 6.6E | Latex Solid Colour Stain | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 39) | 2nd | Latex Solid Colour Stain |
|  |  | 3rd | Latex Solid Colour Stain |
| RIN 6.6F | Latex, (over latex primer) | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  |  | 3rd | Latex |
|  | (DSD 2 or 3 – MPI # 39) |  |  |
| RIN 6.6G | Fire Retardant, Pigmented | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
| RIN 6.6H | Fire Retardant, Clear | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |

RIN 6.7 – FIBERGLASS

| RIN 6.7A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [17] [69]) | 3rd | Latex |
| RIN 6.7B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [17] [69]) | 3rd | Alkyd |
| RIN 6.7C | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # [17] [69]) | 3rd | W. B. Light Industrial Coating |
| RIN 6.7D | Epoxy | 1st | DSD [1] [2] [3] |
|  |  | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 6.7E | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (over epoxy) | 2nd | Polyurethane |
|  | (DSD 2 or 3 – MPI # 77) | 3rd | Polyurethane |
| RIN 6.7F | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  |  | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 6.7G | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # [17] [69]) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 6.7H | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [17] [69]) |  |  |
| RIN 6.7J | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  |  | 3rd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 17]) |  |  |

RIN 6.8 – PLASTIC

| RIN 6.8A | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [17] [69]) |  |  |
| RIN 6.8B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [17] [69]) | 3rd | Alkyd |
| RIN 6.8C | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # [17] [69]) | 3rd | W. B. Light Industrial Coating |
| RIN 6.8D | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # [17] [69]) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 6.8E | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [17] [69]) | 3rd | Latex |
| RIN 6.8F | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # 17) | 3rd | Institutional Low Odor / VOC |
| RIN 6.8G | High Performance Architectural Latex | 1st | Bonding Primer |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (for vinyl wall covering only) |  |  |
| RIN 6.8H | Latex | 1st | Bonding Primer |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (for vinyl wall covering only) | 3rd | Latex |
| RIN 6.8J | Institutional Low Odor / VOC | 1st | Bonding Primer |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (for vinyl wall covering only) | 3rd | Institutional Low Odor / VOC |
| RIN 6.8K | Alkyd | 1st | Bonding Primer |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (for vinyl wall covering only) | 3rd | Alkyd |

RIN 9.1 – SPRAY TEXTURED CEILIING

| RIN 9.1A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level G1 | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [136] [137]) | 3rd | Latex |
| RIN 9.1B | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss level [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [136] [137]) | 3rd | Latex |
| RIN 9.1C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level G1 | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| RIN 9.1D | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [45] [136]) | 3rd | Alkyd |

RIN 9.2 – PLASTER AND GYPSUM BOARD

| RIN 9.2A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | Latex |
| RIN 9.2B | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [50] [137]) |  |  |
| RIN 9.2C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | Alkyd |
| RIN 9.2D | Epoxy | 1st | DSD [1] [2] [3] |
|  | (DSD 2 – MPI # 17) | 2nd | Epoxy |
|  |  | 3rd | Epoxy |
| RIN 9.2E | Epoxy, Water Based | 1st | DSD [1] [2] [3] |
|  | (DSD 2 – MPI # 17) | 2nd | W. B. Epoxy |
|  |  | 3rd | W. B. Epoxy |
| RIN 9.2F | Multicolor | 1st | DSD [1] [2] [3] |
|  | (DSD 1, 2 or 3 – MPI # 125) | 2nd | Multicolor Base coat |
|  |  | 3rd | Multicolor Pattern Coat |
|  |  | 4th | Clear Coat |
| RIN 9.2G | Fire Retardant Coating | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
|  | (clear or pigmented) |  |
| RIN 9.2H | Latex Fire Retardant Coating | (ULC approved), Apply in strict accordance with Manufacturer’s Instructions |
|  | (clear or pigmented) |  |
| RIN 9.2J | Polyurethane, Pigmented | 1st | DSD [1] [2] [3] |
|  | (DSD 2 – MPI # 17) | 2nd | Polyurethane |
|  | (DSD 3 – MPI # 77) | 3rd | Polyurethane |
| RIN 9.2K (Plaster Only) | Latex, (over alkyd primer) | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G2] [G3] [G4] [G5] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # 45) | 3rd | Latex |
| RIN 9.2L | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | W. B. Light Industrial Coating |
| RIN 9.2M | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | Institutional Low Odor / VOC |

RIN 9.3 – ACOUSTIC PANELS AND TILES

| RIN 9.3A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss Level G1 | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | Latex |
| RIN 9.3B | Latex | 1st | DSD [1] [2] [3] |
|  | Gloss level [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [45] [137]) | 3rd | Latex |
| RIN 9.3C | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level G1 | 2nd | Alkyd |
|  |  | 3rd | Alkyd |
| RIN 9.3D | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # [50] [137]) |  | Institutional Low Odor / VOC |
| RIN 9.3E | High Performance Architectural Latex | 1st | DSD [1] [2] [3] |
|  |  | 2nd | HIPAC Latex |
|  | Gloss level [G2] [G3] [G4] [G5] | 3rd | HIPAC Latex |
|  | (DSD 2 or 3 – MPI # [50] [137]) |  |  |

RIN 10.1 – CANVAS AND COTTON COVERINGS

| RIN 10.1A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | Latex |
| RIN 10.1B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # 50) | 3rd | Alkyd |
| RIN 10.1C | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # 50) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |
| RIN 10.1D | Institutional Low Odor / VOC | 1st | DSD [1] [2] [3] |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Institutional Low Odor / VOC |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | Institutional Low Odor / VOC |
| RIN 10.1E | Waterborne Light Industrial Coating | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G3] [G5] [G6] | 2nd | W. B. Light Industrial Coating |
|  | (DSD 2 or 3 – MPI # [50] [137]) | 3rd | W. B. Light Industrial Coating |

RIN 10.2 – BITUMINOUS COATED SURFACES

| RIN 10.2A | Latex | 1st | DSD [1] [2] [3] |
| --- | --- | --- | --- |
|  | Gloss level [G1] [G2] [G3] [G4] [G5] [G6] | 2nd | Latex |
|  | (DSD 2 or 3 – MPI # [50] [107]) | 3rd | Latex |
| RIN 10.2B | Alkyd | 1st | DSD [1] [2] [3] |
|  | Gloss Level [G1] [G3] [G5] [G6] | 2nd | Alkyd |
|  | (DSD 2 or 3 – MPI # [50] [107]) | 3rd | Alkyd |
| RIN 10.2C | Aluminum Paint | 1st | DSD [1] [2] [3] |
|  | (DSD 2 or 3 – MPI # [50] [107]) | 2nd | Aluminum Paint |
|  |  | 3rd | Aluminum Paint |

# END OF SECTION