Section Cover Page

Section 09 96 53 2014-11-01 Vinyl Acrylic Coatings

Refer to “LEED Notes and Credits” page for additional guidance for LEED projects. Delete LEED items if project: .1 is excluded by the Department’s policy on LEED, or .2 the Department has determined that the work of this Contract is not to attain a LEED rating.

This Master Specification Section contains:

.1	This Cover Sheet

.2	LEED Notes and Credits

.3	Specification Section Text:

1.	General

1.1	Related Work Specified in Other Sections

1.2	Product Options and Substitutions

1.3	Reference Documents

1.4	Qualifications

1.5	Submittals

1.6	Delivery, Storage and Handling

1.7	Site Conditions

1.8	Environmental Conditions

1.9	Protection

2.	Products

2.1	Materials

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation/Application

3.3	Clean Up

3.4	Application Schedule

2.	Products

2.1	Materials

2.2	Colours

3.	Execution

3.1	Examination

3.2	Preparation/Application

3.3	Clean Up

3.4	Application Schedule

LEED Notes:

N/A

LEED Credits:

Contribution towards LEED credits in this section may apply as follows:

LEED Credit EQ 4.2 Low-Emitting Materials: Paint and Coatings.

In order to obtain EQ 4.2 protective coatings have to comply with the maximum VOC content limits of the State of California’s South Coast Air Quality Management District (SCAQMD) Rule #1113, Architectural Coatings, January 2004.

1.	General

1.1	RELATED WORK SPECIFIED IN OTHER SECTIONS

.1	[LEED Submittal Forms	Section 01 32 16]

.2	[LEED Requirements	Section 01 35 18]

.3	[Environmental Procedures	Section 01 35 20]

.4	Waste Management and Disposal	Section 01 74 19.

.5	Substrate:	Section [            ].

.6	Sealants:	Section 07 92 00.

.7	Epoxy flooring:	Section 09 67 16.

.8	Painting:	Section 09 91 05.

.9	Epoxy (wall) coating:	Section 09 96 56.

.10	Polyurethane coating:	Section [            ].

.11	Aggregate wall coating:	Section [            ].

1.2	PRODUCT OPTIONS AND SUBSTITUTIONS

.1	Refer to Division 01 for requirements pertaining to product options and substitutions.

1.3	REFERENCE Documents

SPEC NOTE: Edit this article to include only standards referenced within the edited version of this Section, including LEED documentation and sustainable practices.

.1	American Society for Testing and Materials (ASTM)

| .1 | ASTM D1308-02(2007) | Standard Test Method for Effect of Household Chemicals on Clear and Pigmented Organic Finishes |
| --- | --- | --- |
| .2 | ASTM E84-09 | Standard Test Method for Surface Burning Characteristics of Building Materials |
| .3 | ASTM E96/E96M-05 | Standard Test Methods for Water Vapor Transmission of Materials |

.2	Canada Green Building Council (CaGBC)

| .1 | LEED Canada 2009 Rating System | LEED Canada for New Construction and Major Renovations. LEED Canada for Core and Shell Development. Website: www.cagbc.org |
| --- | --- | --- |

.3	Canadian General Standards Board (CGSB):

| .1 | CGSB 1-GP-71 Set of 3 Standards 2003 | Methods of Testing Paints and Pigments - Set includes 1-GP-71 No. 5-96, 1-GP-71 No. 38-96 and 1-GP-71 No. 73-96 |
| --- | --- | --- |

.4	Green Seal (GS)

| .1 | Green Seal Standards GS-11 | Paints, First Edition, May 20, 1993 |
| --- | --- | --- |

.5	South Coast Air Quality Management District (SCAQMD), California State

| .1 | SCAQMD Rule 1113 | June 2006, Paint and Coatings |
| --- | --- | --- |

1.4	QUALIFICATIONS

.1	The work of this Section shall be applied only by experienced applicators of the specified products.

1.5	Submittals

.1	Product Data:

.1	Submit manufacturer’s printed product literature, specifications and data sheets in accordance with Section 01 33 00 - Submittal Procedures.

.2	Submit [two] [          ] copies of Workplace Hazardous Materials Information System (WHMIS) Material Safety Data Sheets (MSDS) in accordance with Section [01 33 00 - Submittal Procedures] [           ]. Indicate VOCs during application [and curing] [           ].

.2	Samples:

.1	Submit 300 x 300 mm representative sample coating in selected colour.  Identify sample by project name including material and colour identification.

.2	Site apply sample installation to minimum 2.0 m2 area, to surface as directed, for approval by the Province.  Retain approved sample until work is completed and accepted.

.3	Sustainable Design Submittals:

SPEC NOTE: Use the following paragraph when LEED Submittals are required.

.1	LEED Submittals: Submit documentation in accordance with Section 01 35 18 – LEED Requirements.  Submit documentation for the following:

.1	Indoor Environmental Quality:

SPEC NOTE: Delete LEED submittal item below if project is not to attain LEED certification or if Credit EQ 4.2 Low Emitting Materials: Paint and Coatings is not being sought. If project is to follow sustainable building practices but not attaining LEED certification, delete references to LEED and retain SCAQMD Rule 1113 and GS-11as a sustainable submittals.

.1	EQ Credit 4.2 - Low-Emitting Materials: Paint and Coatings

1.6	DELIVERY, Storage, and Handling

.1	Delivery and Acceptance Requirements:

.1	Deliver materials undamaged, in original containers, with manufacturer's labels and seals intact.

.2	Storage and Handling Requirements:

.1	Store material in protected conditions with a minimum temperature of 13°C.

.3	Waste Management and Disposal:

.1	Separate waste materials for [reuse] [and] [recycling] in accordance with Section 01 74 19 – Management and Disposal.

1.7	site CONDITIONS

.1	Ambient Conditions:

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could affect coating performance.

.2	For interior coatings:  Minimum surface temperature 10°C 24 hours before, during and 24 hours after application; bright, uniform lighting; broom clean; reasonably dust free.

1.8	ENVIRONMENTAL CONDITIONS

.1	For exterior coatings:  Comply with coating manufacturer's recommendations.  Do not apply under adverse weather conditions which could effect coating performance.

.2	For interior coatings:  Minimum surface temperature 10°C 24 hours before, during and 24 hours after application; bright, uniform lighting; broom clean; reasonably dust free.

1.9	PROTECTION

.1	Protect adjacent surfaces from damage or overspray resulting from work of this Section.  Mask and/or cover adjacent surfaces.  Make good any damage at own expense, to the Province's satisfaction.

.2	Post "Wet Coatings" and "No Smoking" signs, while work is in progress and curing.

2.	Products

2.1	MATERIALS

.1	Emulsion based, vinyl acrylic, mastic coating meeting the following minimum property requirements:

| Property | Test Method | Requirement |
| --- | --- | --- |
| Fire resistance | ASTM E84 | Flame spread 0 Fuel contributed 5 Max. smoke developed 10 |
| Scrubbability | CGSB 1-GP-71 Method 125.1 | No loss of gloss or other deleterious defects for 10,000 cycles |
| Colour fastness | CGSB 1-GP-71 Fademeter | No colour change after 48 hours |
| Impact resistance | CGSB 1-GP-71 Method 147.1 Gardner | Unaffected at 1.1 J 9.0 J min. |
| Water vapour | ASTM E96 | 0.3 metric perms max |
| Toxicity | Canadian Dept. of Agriculture | Approved nontoxic |
| Stain resistance | ASTM D1308 | Not affected by common acids, hydroxides, salts and household cleaning agents |

SPEC NOTE:  The above material is used in wet or high humidity conditions or where coating is steam cleaned.  The following materials meet the above requirements:   Duroplast 300, by Duochem.

2.2	COLOURS

.1	[One] [Two] [     ] colours will be selected by Province from manufacturer's standard range.

OR

.1	Refer to Application Schedule.

3.	Execution

3.1	EXAMINATION

.1	Examine all surfaces conditions to which the work of this Section is to be applied.  Report any deficient surfaces to the Province.

3.2	PREPARATION/APPLICATION

.1	Prepare surfaces and apply as directed in the manufacturer's literature.

.2	Match finished work to approved samples, maintain uniform in thickness, sheen, colour, texture and free from defects detrimental to appearance or performance.

.3	Minimum cured thickness of applied material to be 380 micrometres.

3.3	CLEANUP

.1	Promptly, as the work proceeds and upon completion, clean up excess materials and rubbish.

3.4	APPLICATION SCHEDULE

| Room No./Name | Finish | [Colour] |
| --- | --- | --- |
| [ ] | [satin] [semi-gloss] [tile-like] | [ ] |
| [ ] | [ ] | [ ] |
| All other locations scheduled to receive vinyl acrylic coating | [ ] | [ ] |

END OF SECTION